## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | SHELL | - | Carbon Steel | SA-516 | 70 | No | 80 C | 10 BAR | LOW | 
- | PLATE HEAD | - | Carbon Steel | SA-516 | 70 | No | 80 C | 10 BAR |  | 
- | DISH HEAD | - | Carbon Steel | SA-516 | 70 | No | 80 C | 10 BAR |  | 
- | BAR | - | Carbon Steel | SA-106 | B | No | 80 C | 10 BAR |  | 
- | HALF COUPLING | - | Carbon Steel | SA-105 | - | No | 80 C | 10 BAR |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | FULL COUPLING | - | Carbon Steel | SA-105 | - | No | 80 C | 10 BAR | LOW | 
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion