## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) | LOW | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Not Found | SA-179 | - | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-106 | Gr. B | - | 150 DEG. C | 10.00 kg/cm2 (g) | LOW | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-106 | Gr. B | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) | LOW | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Stainless Steel Bolting | SA-193 | Gr. B7 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Heavy Hex Nuts | SA-194 | Gr. 2H | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 4
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Not Found | SA-36 | - | - | 150 DEG. C | 10.00 kg/cm2 (g) | LOW | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Not Found | SS-316 | - | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Stainless Steel Bolting | SA-193 | Gr. B7 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Heavy Hex Nuts | SA-194 | Gr. 2H | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Not Found | Non Asbestos | - | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 5
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-106 | Gr. B | - | 150 DEG. C | 10.00 kg/cm2 (g) | LOW | 
- | METHANOL (SHELL) / WATER (TUBE) | - | Carbon Steel | SA-516 | Gr. 70 | - | 150 DEG. C | 10.00 kg/cm2 (g) |  | 
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion