## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | Shell Plate | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar | LOW | 
- | 2:1 Ellipsoidal Head | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
- | Lifting Lug | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
- | Lifting Lug | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
- | Saddle Plate | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Saddle Baseplate | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar | LOW | 
- | Saddle Baseplate | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
- | Saddle Baseplate | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar | LOW | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 4
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar | LOW | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar |  | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 5
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Neck | - | Stainless Steel | ASTM A312 | TP304L | - | 90 °C | 1 Bar | LOW | 
- | Blind Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Spiral Wound Gasket | - | Not Found | ASME B16.20 | DN600 | - | 90 °C | 1 Bar |  | 
- | Flange | - | Stainless Steel | ASTM A182 | F304L | - | 90 °C | 1 Bar |  | 
- | Neck | - | Stainless Steel | ASTM A240 | 304L | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 6
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Stud Bolt | - | Stainless Steel Bolting | ASTM A193 | GR B8M | - | 90 °C | 1 Bar | LOW | 
- | Nuts & Washer | - | Heavy Hex Nuts | ASTM A194 | GR 2H | - | 90 °C | 1 Bar |  | 
- | Bracket 1 | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Angle Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Bracket 2 | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 7
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Bracket 3 | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar | LOW | 
- | Grating | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Angle Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Angle Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Flat Plate | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 8
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Flat Plate | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar | LOW | 
- | Angle Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Angle Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Side Rail | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Ladder Bracket | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 9
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Round Bar | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar | LOW | 
- | Saddle Support Plate | - | Stainless Steel | ASTM A240 | J304L | - | 90 °C | 1 Bar |  | 
- | Pad Plate | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | Pad Plate | - | Not Found | ASTM A36 | - | - | 90 °C | 1 Bar |  | 
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion