## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | PLATE 1571x600x5mm SHELL TO BE ROLLED | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.0 BarG | LOW | 
- | DISH HEAD 8 THK TO BE FORMED 1D 2:1 TYPE | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.0 BarG |  | 
- | SEAMLESS PIPE DN50 x 87 SCH 40S | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
- | SEAMLESS PIPE DN25 x 100 SCH 40S | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
- | SEAMLESS PIPE DN50 x 112 SCH 40S | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | FLANGE DN50 CLASS 150 WNRF SCH 40S | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG | LOW | 
- | FLANGE DN25 CLASS 150 WNRF SCH 40S | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG |  | 
- | FLANGE DN50 CLASS 150 WNRF SCH 40S | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG |  | 
- | BASE PLATE 150 x 150 x 5 THK | - | Stainless Steel | SA 240 M | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | LIFTING LUG PLATE 190 x 80 x 6 THK | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.0 BarG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | DOUBLER PLATE 120 x 150 x 12.7 THK | - | Stainless Steel | SA 240 M | Gr. 304 | - | 100 °C | 1.0 BarG | LOW | 
- | EQUAL ANGLE BAR 3" x 3" x 1/4" THK | - | Stainless Steel | SA 240 M | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | EARTHING LUG | - | Stainless Steel | SA 240 M | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion