## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | Shell & Dished End | - | Carbon Steel | SA-516 | 70 | - | 185°C | 1000 kPaG | LOW | 
- | Flange, Manhole Flange and Cover | - | Carbon Steel | SA-105 | - | - | 185°C | 1000 kPaG |  | 
- | Pipe | - | Carbon Steel | SA-106 | Gr.B | - | 185°C | 1000 kPaG |  | 
- | Socket | - | Carbon Steel | SA-105 | - | - | 185°C | 1000 kPaG |  | 
- | Reinforced Plate | - | Carbon Steel | SA-516 | 70 | - | 185°C | 1000 kPaG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | Legs | - | Structural Steel | S275JR | - | - | 185°C | 1000 kPaG | LOW | 
- | Bolt & Nut (Pressure Retaining) | - | Stainless Steel Bolting | SA-193 / SA-194 | B7 / 2H | - | 185°C | 1000 kPaG |  | 
- | Bolt & Nut (External Fittings) | - | Carbon Steel | JIS G3507 | - | - | 185°C | 1000 kPaG |  | 
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion