## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
DMSO | Shell | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.0 BarG | LOW | 
DMSO | Head | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.0 BarG |  | 
DMSO | Pipe (Nozzle N5A/N5B) | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
DMSO | Pipe (Nozzle N3/N4) | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
DMSO | Pipe (Nozzle N1/N2) | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.0 BarG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion
Air Receiver
V-001
MLK_PMT_10102_-_V-002

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
DMSO | Flange (for DN50 nozzles) | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG | LOW | 
DMSO | Flange (for DN25 nozzles) | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG |  | 
DMSO | Flange (for DN150 nozzles) | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.0 BarG |  | 
DMSO | Doubler Plate (Nozzle Reinforcement) | - | Stainless Steel | SA 240 M | Gr 304 | - | 100 °C | 1.0 BarG |  | 
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion
Air Receiver
V-001
MLK_PMT_10102_-_V-002
Air Receiver
V-001
MLK_PMT_10102_-_V-002