## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.1 Bar G | LOW | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.1 Bar G |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | 100 °C | 1.1 Bar G | LOW | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G | LOW | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 4
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G | LOW | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G |  | 
- | - | - | Stainless Steel | SA 240 M Gr. | 304L | - | 100 °C | 1.1 Bar G |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion