## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 7, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 7, dtype: object | LOW | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 8, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 8, dtype: object |  | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 9, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 9, dtype: object |  | 
- | - | - | Stainless Steel | SA 240 M | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 10, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 10, dtype: object |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 11, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 11, dtype: object |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 12, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 12, dtype: object | LOW | 
- | - | - | Stainless Steel | SA 312 M TP | 316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 13, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 13, dtype: object |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 14, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 14, dtype: object |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 15, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 15, dtype: object |  | 
- | - | - | Stainless Steel | SA 182 M | F316L | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 16, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 16, dtype: object |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | - | - | Stainless Steel | SA 240 M | Gr. 304 | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 17, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 17, dtype: object | LOW | 
- | - | - | Stainless Steel | SA 240 M | Gr. 304 | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 18, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 18, dtype: object |  | 
- | - | - | Stainless Steel | SA 240 M | Gr. 304 | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 19, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 19, dtype: object |  | 
- | - | - | Stainless Steel | SA 240 M | Gr. 304 | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 20, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 20, dtype: object |  | 
- | - | - | Stainless Steel | SA 240 M | Gr. 304 | - | TEMP. (°C) 100 °C TEMP. (°C) 100 °C Name: 21, dtype: object | PRESSURE (MPA) 1.1 BarG PRESSURE (MPA) 1.0 BarG Name: 21, dtype: object |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion