## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
1 | PLATE 1571x600x5mm SHELL TO BE ROLLED | - | Stainless Steel | SA 240 | 316L | - | 100 °C | 1.0 BarG | LOW | 
- | DISH HEAD 8Thk TO BE FORMED 2:1 TYPE | - | Stainless Steel | SA 240 | 316L | - | 100 °C | 1.0 BarG |  | 
- | SEAMLESS PIPE DN50 X 8T SCH 40s | - | Stainless Steel | SA 312 | TP 316L | - | 100 °C | 1.0 BarG |  | 
- | SEAMLESS PIPE DN25 X 100 SCH 40s | - | Stainless Steel | SA 312 | TP 316L | - | 100 °C | 1.0 BarG |  | 
- | FLANGE DN50 CLASS 150 WNRF SCH 40s | - | Stainless Steel | SA 182 | F316L | - | 100 °C | 1.0 BarG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 2
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | FLANGE DN25 CLASS 150 WNRF SCH 40s | - | Stainless Steel | SA 182 | F316L | - | 100 °C | 1.0 BarG | LOW | 
- | FLANGE DN150 CLASS 150 WNRF SCH 40s | - | Stainless Steel | SA 182 | F316L | - | 100 °C | 1.0 BarG |  | 
- | BASE PLATE 150 X 150 X 5Thk | - | Stainless Steel | SA 240 | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | LIFTING LUG PLATE 120 X 80 X 6Thk | - | Stainless Steel | SA 240 | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | DOUBLER PLATE 120 X 150 X 12.7Thk | - | Stainless Steel | SA 240 | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion

## Slide 3
FLUID | COMPONENT | DESIGN CODE | MATERIAL |  |  | INSULATED (Y/N) | OP. PARAMETER |  | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell General Corrosion External ATMOSPHERIC CORROSION
 |  |  | TYPE | SPEC | GR |  | T (֯C) | P (Mpa) |  | 
- | EQUAL ANGLE BAR 3" X 3" X 1/4" Thk | - | Stainless Steel | SA 240 | Gr. 304 | - | 100 °C | 1.0 BarG | LOW | 
- | EARTHING LUG | - | Stainless Steel | SA 240 | Gr. 304 | - | 100 °C | 1.0 BarG |  | 
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
- | - | - | - | - | - | - | - | - | - | -
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) With follow up by UT, RT, or pit gauge as required. | Atmospheric Corrosion